Table captions

Table 1

Structural parameters of the first coordination shells around Bi atom in Bi0.2Nd0.8VO4 and around Nd in NdVO4, respectively. R = distance and σ2 = Debye-Waller factor. Uncertainty of the last digit is given in parentheses. The fitting statistics R-factor was 0.0018 for the Bi fit and 0.005 for the Nd fit. The amplitude reduction factor was S02= 0.98 ± 0.09 for Bi and 0.94 ± 0.07 for Nd. The shift of the energy origin, ΔE0 was -4 ± 1 eV for Bi and 3.7 ± 0.8 eV for Nd.

| Neighbour element of |  | Number of neighbours of |  | R [Å] |  | σ2 [Å2] |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Bi in Bi0.2Nd0.8VO4 | Nd in NdVO4 | Bi in Bi0.2Nd0.8VO4 | Nd in NdVO4 | From Bi in Bi0.2Nd0.8VO4 to | From Nd in NdVO4 to | Bi in Bi0.2Nd0.8VO4 to | Nd in NdVO4 to |
| O V Nd V |  | 8 2 4 4 |  | 2.39(1) | 2.44(1) | 0.019(1) | 0.010(1) |
|  |  |  |  | 3.20(1) | 3.22(1) | 0.008(1) | 0.004(1) |
|  |  |  |  | 3.99(1) | 4.00(1) | 0.013(1) | 0.008(1) |
|  |  |  |  | 3.99(1) | 4.00(1) | 0.016(1) | 0.010(1) |

Table 2

Structural parameters of the first coordination shells around Nd atom in the Bi0.5Nd0.5VO4 model structure. R = distance and σ2 = Debye-Waller factor. Uncertainty of the last digit is given in parentheses. The fitting statistics, R-factor= 0.007. The amplitude reduction factor S02 = 0.8 ± 0.1, and the shift of the energy origin ∆E0 = 1.3 ± 1.5 eV.

| Neighbour element of Nd | Number of neighbours | R [Å] | σ2 [Å2] |
| --- | --- | --- | --- |
| O | 8 | 2.43(1) | 0.008(1) |
| V | 2 | 3.15(2) | 0.007(2) |
| Nd | 2 | 3.92(2) | 0.003(2) |
| V | 4 | 3.92(2) | 0.011(2) |
| Bi | 2 | 4.22(3) | 0.003(2) |
| O | 12 | 4.31(2) | 0.015(5) |
| O | 8 | 5.06(7) | 0.011(1) |

- Table 3

- Experimental band-gap energy values for NdVO4.

| - Paper | - Experimental Eg [eV] | - Synthesis method and particle size |
| --- | --- | --- |
| - Panchal V et al. [39] | - 3.72 | - Single crystals, ~ 80µm |
| - This work | - 3.53 | - Solid-state synthesis, ~1 µm |
| - Mahapatra S et al. [40] | - 2.99 | - Co-precipitation, 200 nm particles |
| - Xu J et al. [51] | - 2.95 | - Molten salt method, 100 nm diameter and up to 3 µm length nanowires |
| - Kalai Selvan R et al. [52] | - 2.15 | - Sonochemical synthesis, 20 nm rods |