## Slide 1: HV-CMOS
Ivan Peric
for ATLAS and CLIC HVCMOS R&D and Mu3e Collaborations

## Slide 2: HVCMOS introduction
Ideas:
Use the standard (HV)CMOS technologies to implement particle detectors
Use a high voltage to deplete the sensor volume – charge collection by drift
The standard implementation: CMOS electronics inside the deep n-well-collecting electrode
“Smart diode”
Partial depletion from the top, no backside electrode needed
Deep-n-well
PMOS
NMOS
N-Well
P-Substrate
Shallow-p-well
Shallow-n-well
~60V

## Slide 3: HVCMOS introduction
Some drawbacks:
The standard substrates are relatively low resistive (~20 Ωcm)
The depleted region is up to ~15 µm thick – MIP signals are relatively weak ~ 1800 e
The collection electrode is, at the same time, the PMOS bulk – there is a strong capacitive crosstalk from PMOS transistors to the detector input.
General drawback of monolithic sensors: Complex in-pixel electronics leads to increased detector capacitance or to decreased electrode-/pixel-size ratio
Deep-n-well
PMOS
NMOS
N-Well
P-Substrate
Shallow-p-well
Shallow-n-well
~60V

## Slide 4: HVCMOS detector types
We investigate two detector structures:
A) Hybrid detector with a “smart” HVCMOS sensor and the capacitive signal transmission to the readout ASIC (capacitively coupled pixel sensor - CCPD)
B) Monolithic pixel detector with digital signal processing on the chip periphery
One RO cell
/pixel
Pixel contains a charge sensitive amplifier
CSA
+
A)
B)

## Slide 5: HVCMOS detector types
CCPD
ATLAS-pixel “style”: the digital outputs of three pixels are multiplexed to one pixel readout cell
HVCMOS pixel contains an amplifier and a comparator
CLIC “style”: every HVCMOS pixel has its own readout cell
HVCMOS pixel contains only an amplifier
+
TOT = sub pixel address
Readout pixel
Readout pixel
Size: 50 µm x 250 µm
Size: 33 µm x 125 µm
Size: 25 µm x 25 µm
Size: 25 µm x 25 µm
Different logic 1 levels

## Slide 6: Monolithic HVCMOS pixel sensor for Mu3e experiment

## Slide 7: Monolithic HVCMOS pixel sensor for Mu3e experiment
RAM/ROM
Hit flag
Priority scan logic
Time stamp
Data bus
Read
Row/Col Addr + TS
One RO cell
/pixel
Readout cell function – time stamp is stored when hit arrives
Hit data are stored until the readout
Priority logic controls the readout order
RO cell size in 0.18 µm AMS technology ~ 7 µm x 40 µm
(with comparator and threshold-tune DAC)
Comparator
and Thr tune DAC
Pixel contains a charge sensitive amplifier
CSA
Comparator
Concept: Every pixel has its own readout cell, placed on the chip periphery

## Slide 8: Monolithic HVCMOS pixel sensor for Mu3e experiment
92µm
3 mm
Readout cell
One pixel

## Slide 9: MuPixel (readout-cell)
TS DRAM
Address ROM
CMOS digital part
Comparator
Coupling capacitor
DAC and SRAM
7µm
46 µm

## Slide 10: MuPixel test beam
Test-beam measurement February 2014 DESY
Performed by our colleagues from Institute for Physics in Heidelberg
Result analysis: Moritz Kiehn, Niklaus Berger, et al.

## Slide 11: MuPixel test beam
Test-beam measurement February 2014 DESY
Performed by our colleagues from Institute for Physics in Heidelberg
Result analysis: Moritz Kiehn, Niklaus Berger, et al.
80ns
Probably caused by indirect hits

## Slide 12: Periphery area estimation for triggered readout
RAM/ROM
Hit flag
Priority scan logic
Time stamp
Data bus
Read
One RO cell
/pixel
Global readout
Periphery size ~ 2.5 %
Delayed TS and trigger
Readout cell function – time stamp is stored when hit arrives
The stored time stamp is compared with the current time stamp
If trigger arrives with the correct latency, the triggered hit flag is set
Priority logic controls the readout order
Estimated cell size in 0.18 µm AMS technology without comparator ~ 7 µm x 50 µm
Example: Pixel size 50 µm x 250 µm
Chip size: ~ 2 cm x 2 cm
Number of pixels: 400 x 80
Size of periphery without comparator:
2 cm x 560 µm (~ 2.5%)
Triggered hit flag
Pixel contains a charge sensitive amplifier and a discriminator with threshold tune DAC
CSA
Comparator
Concept: Every pixel has its own readout cell, placed on the chip periphery

## Slide 13: HVCMOS pixel sensor for ATLAS

## Slide 14: CCPD detector (HV2FEI4)
The digital outputs of three pixels are multiplexed to one pixel readout cell
2
3
1
2
3
1
CCPD Pixels
+
Size: 50 µm x 250 µm
Size: 33 µm x 125 µm
Different logic 1 levels

## Slide 15: HV2FEI4
“Sub-pixel resolution” by measuring of time over threshold (measurement: Malte Backhaus)
2
3
1
2
3
1
CCPD Pixels

## Slide 16: HV2FEI4: segmented strip measurements
Analog encoding of pixels positions in the case of the segmented strip readout
Amp
Monitor
Chip
Oscilloscope
Th1
Fe55
Absorber

## Slide 17: HV2FEI4: neutron irradiation 1015 neq/cm2
No evidence of signal decrease after 1015 neq/cm2

## Slide 18: HV2FEI4: x-ray irradiation to 862 Mrad
A detector has been irradiated to 862 Mrad with x-rays. (chips on during the irradiation, 2 hours of annealing at 70C after each 100Mrad)
862 Mrad
90e
150e

## Slide 19: HV2FEI4: test beam
Test beam DESY, analysis: Lars Graber, et al.
Threshold tune not optimal
(changed in the new version)

## Slide 20: Further steps
We need to improve time walk
We need to improve SNR of CCPDs for ATLAS, especially after irradiation
Three strategies:
1) optimize present design
2) invent more clever electronics
3) improve the detector structure and technology

## Slide 21: Detector structure improvements

## Slide 22: Isolated PMOS
Detector structure improvements:
Isolated PMOS
Eliminates PMOS to sensor crosstalk, allows more freedom when pixel electronics is designed
NMOS
PMOS
3.3V
NMOS
PMOS
Improvement:
Deep n-well
Deep p-well
Shallow n-well

## Slide 23: High resistive substrates
Detector structure improvements:
High resistive substrates
Deep-n-well
+-
+-
+-
+-
+-
+-
+-
+-
Depleted 12 µm
12 um
Primary signal
100%-Signal collection: drift
Secondary signal
Partial signal collection: diffusion
+-
+-
+-
+-
+-
+-
Signal loss: recombination
Signal loss
Deep-n-well
+-
+-
+-
+-
+-
+-
+-
+-
Depleted 24µm
(@ equal bias voltage)
Depleted 48µm
(@ equal field, doubled bias voltage)
Primary signal
100%-Signal collection: drift
+-
+-
+-
+-
+-
+-
Particle
Particle
Uniformly doped substrate 20 Ω cm
Signal 1800e (50%-50% drift-diffusion)
Uniformly doped substrate 80 Ω cm
Signal: ~ 2700e-4500e (estimation)

## Slide 24: High resistive substrates
Detector structure improvements:
High resistive substrates
These improvements are possible within AMS- and LFoundry processes
Deep-n-well
+-
+-
+-
+-
+-
+-
+-
+-
Depleted 12 µm
12 um
Primary signal
100%-Signal collection: drift
Secondary signal
Partial signal collection: diffusion
+-
+-
+-
+-
+-
+-
Signal loss: recombination
Signal loss
Deep-n-well
+-
+-
+-
+-
+-
+-
+-
+-
Depleted 24µm
(@ equal bias voltage)
Depleted 48µm
(@ equal field, doubled bias voltage)
Primary signal
100%-Signal collection: drift
+-
+-
+-
+-
+-
+-
Particle
Particle
Uniformly doped substrate 20 Ω cm
Signal 1800e (50%-50% drift-diffusion)
Uniformly doped substrate 80 Ω cm
Signal: ~ 2700e-4500e (estimation)

## Slide 25: AMS TSV process

## Slide 26: TSV – bask side RDL
nwell
Transistor
M1
M3
M4
RDL
(MET4_TSV)
Wire bond
Bump
Wire bond pad
(PAD_TSV)
VIAT_TSV
Read out Chip
CMOS Side
Sensor
Backside RDL
AMS offers through silicon vias and wafer bonding (so far only for H35, from end of 2015 for H18 as well)
Backside redistribution layer and backside pads are possible
TSV pitch 260 µm
Very important for the module construction

## Slide 27: Pixel detectors
…
Readout chip
Detector as it is done now:
Diode based pixel sensor bump-bonded to readout ASICs
Present development:
CMOS pixel sensor capacitively coupled to readout ASICs
With TSVs
CMOS pixel sensor with backside contacts
capacitively coupled to readout ASICs
PCB
Pixel sensor
(diode based)
(e.g. 8 x 2cm)
CMOS pixel sensor
several reticles
(e.g. 4 x 2 cm)
Readout chip
Pixel sensor
Readout chips
Wire bond for sensor bias
Wire bonds for RO chips
Wire bonds for RO chips
Wire bonds for sensor chip
Readout chips
CMOS pixel sensor
Capacitive signal transmission
CMOS pixel sensor
several reticles
(e.g. 4 x 2 cm)
Readout chip
Wire bonds for sensor chip
Wire bonds for RO chips
CMOS pixel sensor with backside contacts
TSVs
Backside contact
PCB
PCB
PCB
Capacitive signal transmission

## Slide 28: Summary
Collaborations have been formed with the goals to develop HVCMOS sensors for ATLAS- and Mu3e experiments, as well for CLIC
The Mu3e prototype detector (technology AMS 0.18 µm H18) (design Heidelberg) is a fully monolithic sensor with untriggered time-stamp based readout
Detection efficiency of >99% has been measured in a beam test, time resolution (time walk) is ~ 70 ns.
The ATLAS prototypes in AMS 0.18 µm (H18) (design HD) and GF 0.13 µm (design CPPM, HD) technologies are capacitively coupled smart sensors that can be readout using FE-I4 chip
Irradiations and test beam measurements have been performed on the H18 chip
The H18-chip is operational after 880 MRad and 1016 neq/cm2
A test beam measurement has been performed with the test-setups which are still not optimized and in development stage – the threshold uniformity was poor
The uniradiated H18-detector had a detection efficiency of >90% in the regions with lower threshold

## Slide 29: Summary
We need to improve the time walk and the detection efficiency
Three approaches:
1) Optimization of the present design
2) Use of low-pass filter and the time-walk compensation circuit
3) Detector structure improvements (isolated PMOS) and the use of substrates of higher resistivity
Chip producers AMS and LFoundry allow such “extra features” within their processes
AMS additionally offers through silicon vias and wafer bonding (so far only for H35, from end of 2015 also for H18 process)
We are also investigating the use of HVCMOS sensors (segmented strips) for the ATLAS strip layers
Constant delay lossy multiplexing can be used – every hit is transmitted to one of n outputs with a constant delay of ~60 ns.
Hit loss occurs only if there are more than n simultaneous hits within one bunch crossing

## Slide 30: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2

## Slide 31: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2

## Slide 32: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2
0
1
2

## Slide 33: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2
0
1
2
A
B

## Slide 34: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2

## Slide 35: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2

## Slide 36: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2
0
1
0

## Slide 37: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2
0
1
0
C

## Slide 38: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2

## Slide 39: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2

## Slide 40: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2
0
1
2

## Slide 41: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2
0
1
2
A
D

## Slide 42: Segmented strip detector with lossy constant-delay-multiplexing
A
C
D
B
Output 1
Output 2

## Slide 43: Time Walk Compensation

## Slide 44: Time Walk Compensation
The idea: Adding of low-pass filter decreases the noise without increasing the power consumption
=> Better SNR, lower threshold
However: a slow output signal leads to a time-walk
Time walk is caused 1) by the fluctuations of the input signal and 2) by the low and signal-dependent response speed of the electronics
Can we compensate for time walk, without decreasing the shaping time constants?
Iamp
Cdet
Tsha
TW
Tsha
Th
Sig

## Slide 45: Time Walk Compensation
Imagine a comparator which has the output zero-to-one transition speed, that depends on the input signal “overdrive”
High amplitude signal – faster threshold crossing but slower 0-1 transition
Low amplitude signal – slower threshold crossing but faster 0-1 transition
Result: the threshold-crossing- and the transition time skews compensate each other
Second comparator generates time-walk free signal
Slow down
Slow down
Higher amplitude
Lower amplitude
2

## Slide 46: Time Walk Compensation – AMS 350 nm
TW 62ns
3600e
900e
Max 3600e:468ns
Max 900e:408ns
TW 62ns
Noise=8.8mV, Thr=55mV, Bias current=10µA, Pixel size = 50x250µm, Ifoll=10, amplifier power 200mW/cm2
Shaper Output

## Slide 47: Time Walk Compensation – AMS 350 nm
TW 4ns
3600e
900e
Noise=8.8mV, Thr=55mV, Bias current=10µA, Pixel size = 50x250µm, Ifoll=10, amplifier power 200mW/cm2
Comparator Output

## Slide 48: Time Walk Compensation
3600e
900e
TW 75ns
Noise=8.0mV, Thr=55mV, Bias current=10µA, Pixel size = 50x500µm, Ifoll=7, amplifier power 100mW/cm2
Shaper Output

## Slide 49: Time Walk Compensation
TW 5ns
3600e
900e
Noise=8.0mV, Thr=55mV, Bias current=10µA, Pixel size = 50x500µm, Ifoll=7, amplifier power 100mW/cm2
Comparator Output

## Slide 50: Time Walk Compensation
3600e
900e
TW 116ns
Noise=7.9mV, Thr=55mV, Bias current=5µA, Pixel size = 50x500µm, Ifoll=5, amplifier power 50mW/cm2
Shaper Output

## Slide 51: Time Walk Compensation
TW 8ns
3600e
900e
Noise=7.9mV, Thr=55mV, Bias current=5µA, Pixel size = 50x500µm, Ifoll=5, amplifier power 50mW/cm2
Comparator Output