Functionalization of MWCNTs with Atomic Nitrogen
Benoit Ruelle1,2, Alexandre Felten3, Jacques Ghijsen3, Wolfgang Drube4, Robert L. Johnson4,5, Duoduo Liang6, Rolf Erni6, Gustaaf Van Tendeloo6, Philippe Dubois2, Michel Hecq1, and Carla Bittencourt1,

1) LCIA, University of Mons-Hainaut, B-7000 Mons, Belgium
2) SMPC, University of Mons-Hainaut, B-7000, Belgium

3) Lab. Electron Spectroscopy (LISE), FUNDP, B-5000 Namur, Belgium 
4) DESY, Hasylab, D-22603 Hamburg, Germany

5) Institut für Experimentalphysik, Hamburg University, D-22761 Hamburg, Germany

6) EMAT, University of Antwerp, B-2020 Antwerp, Belgium
Keywords: CNTs, Chemical Functionalization, Photoelectron Spectroscopy, Plasma, Surface Treatment, High Resolution Microscopy, Synchrotron Radiation
Abstract:

In this study of the changes induced by exposing MWCNTs to a nitrogen plasma, it was found by HRTEM that the atomic nitrogen exposure does not significantly etch the surface of the CNT. Nevertheless, the atomic nitrogen generated by a microwave plasma effectively grafts amine, nitrile, amide, and oxime groups onto the CNT surface, as observed by XPS, altering the density of valence electronic states, as seen in UPS.
Introduction

Carbon nanotubes (CNTs) are being considered for several applications such as transistors or gas sensors (Ciraci et al., 2004), for which their surface reactivity and electrical and/or mechanical properties must be tailored by adding atoms or molecules to the side walls (Collins et al., 2000). Functionalization is often accomplished by immersing the nanotubes in appropriate chemical solutions or exposing them to vapours at high temperatures (Ciraci et al., 2004). By contrast, a cold plasma treatment has the advantage of being clean and providing a wide range of different functional groups depending on the parameters used to generate the plasma (Ruelle et al., 2007, Khare et al., 2004, and Felten et al., 2005). 

To study the influence of grafting nitrogen atoms onto CNT surfaces, multi-walled carbon nanotubes (MWCNTs) were exposed to atomic nitrogen generated by dissociating molecular nitrogen in an Ar + N2 microwave (MW) plasma (Ruelle et al., 2007). High-resolution transmission (HRTEM) and scanning (SEM) electron microscopy were used to investigate the surface morphology. The resulting modification of the electronic structure of the CNT was investigated by X-ray and ultra-violet photoelectron spectroscopy.
Experiments
Samples were prepared using commercial MWCNT (NC7000) supplied by Nanocyl S.A. Functionalization was performed in the post-discharge chamber of an Ar+N2 microwave plasma (2.45 GHz), the details of which were published by Ruelle et al. (2007). The average discharge power was set to 400 W with a flow ratio of Ar to N2 equal to 14:1. The samples were prepared by exposing the CNTs to the plasma for three different treatment times: 5, 15 and 45 minutes and were kept in the air until they were introduced in the electron microscope or the photoelectron spectrometer.
Depending on the subsequent analysis method, the MWCNT powder was mounted on different supports before plasma treatment. For photoemission analysis, it was supported on a conductive adhesive tape compatible with ultra-high vacuum. The samples for the TEM analysis were first dissolved in ethanol and dropped on a honeycomb film supported by a copper grid.

Photoemission measurements were performed in Hasylab. X-ray photoemission measurements (XPS at a photon energy of 3300 eV) were performed on the BW2 beamline, described in details by Drube et al. (1995 and 1998). Ultra-violet photoelectron spectroscopy (UPS) experiments were performed at the FLIPPER II beamline (Johnson and Reichardt, 1983), using a photon energy of 110 eV, the overall resolution of the system (source + analyser) was 0.2 eV. Binding energies were calibrated with respect to the 4f level (in the case of XPS) or to the Fermi edge (in the case of UPS) of a continuous thick evaporated gold film. 

High-resolution transmission electron microscopy (HRTEM) was carried out using a Philips CM30 FEG instrument operated at 300 kV. In addition, scanning electron microscopy was performed using a JEM-5510 instrument.

Results and Discussion

The samples were analysed by HRTEM and SEM to evaluate the possible etching of CNT walls due to exposure to atomic nitrogen. Figures 1 and 2 show respectively typical SEM and HRTEM images recorded from a treated sample after 45 minutes in the Ar + N2 microwave plasma. The excellent condition of the walls of the CNTs indicates that, for the chosen parameters, the plasma treatment does not damage the CNT surface.
X-ray photoelectron spectroscopy was used to evaluate the chemical nature of the CNT surface after exposure to atomic nitrogen. Figure 3 shows the comparison of XPS spectra recorded on pristine CNTs and on N-functionalized CNTs. The peak at 284.3 eV binding energy, observed in both spectra, arises from photoelectrons emitted from the C 1s core level. The presence of the peak near 399 eV, in the spectrum recorded on the nitrogen-plasma treated sample, proves the effective grafting of nitrogen (Beamson and Briggs, 1992). Figure 4 shows a comparison between the C 1s peaks recorded from pristine and treated MWCNTs. The chemical modification produced by the plasma treatment is revealed by the new broad structure near 287.5 eV that is attributed to photoelectrons emitted from carbon atoms belonging to amine, nitrile, amide, and oxime groups (Ruelle et al., 2007, Khare et al., 2004, and Felten et al., 2005).
The changes in the valence electronic states are revealed by Fig. 5, which summarizes the ultraviolet photoelectron spectroscopy valence band spectra obtained from four different samples: pristine MWCNTs and MWCNTs exposed to atomic nitrogen for 5 minutes, 15 minutes and 45 minutes. The valence band spectra were recorded at a photon energy of 110 eV. The characteristic features arising from the threefold coordination of the C atoms are the 2p-π band near 3.5 eV, the 2p-σ states near 5.5 and 8.0 eV, and the mixed 2s-2p hybridized states at 13.6 eV. The feature near 14 eV was reported by Lim et al. (2002) to be related to oxygen molecules physisorbed on the wall and at the edges of the MWCNTs. In addition to the features observed in the UPS valence band spectrum recorded on the pristine CNTs reference sample, spectra recorded after the N-treatment have a band peaking near 4.2 eV that was attributed to photoelectrons emitted from nitrogen lone pair states (sp2 hybridized nitrogen) (Björkqvist et al, 1998 and Lim et al., 2002). The dominant feature centred at 8.5 eV contains contributions from C and N 2p electrons associated with π bonds overlapping the σ-bond feature of the C 2p electrons located at about 7.5 eV (see Fig. 5, pristine sample). The band located at 9.8 eV is generated by photoelectrons emitted from C 2p – N 2p σ-states (Chen et al., 1999 and Hammer et al., 2000). A small quantity of oxygen was observed to be grafted onto the CNT surface (the oxygen relative atomic concentration derived from XPS was 2.8 %). It may originate either from the residual gas in the plasma chamber or during the ex situ sample preparation. 
Conclusion
Photoelectron spectroscopy analysis showed that by exposing MWCNTs to atomic nitrogen generated in a microwave plasma, nitrogen chemical groups can be grafted onto the CNT surface altering the density of electronic states. After the plasma treatment, the 2p-π states can no longer be observed and the contribution of 2p-σ states is enhanced. This suggests that the chemical groups introduced by treating CNTs in the post-discharge zone of a microwave Ar+N2 plasma contribute to the 2p-σ states. The HRTEM and SEM images reveal that the atomic nitrogen plasma does not damage the surface of the CNTs.
Acknowledgements
This work is financially supported by the Belgian Program on Interuniversity Attraction Pole (PAI 6/1 and PAI 6/27), Nano2hybrids (EC-Strep -033311) and by DESY and the European Commission under contract RII3-CT 2004-506008 (IASFS). JG is research associate of NFSR (Belgium). This work is partially supported by the “Fonds pour la formation à la Recherche dans l’Industrie et dans l’Agriculture (FRIA)”. The authors are very grateful to Nanocyl S.A. (Sambreville,Belgium) for the kind supply of the carbon nanotubes samples.

References
Beamson G., Briggs D., 1992. High Resolution XPS of Organic Polymers: The Scienta 300 Database. Wiley, Chichester.
Björkqvist M., Göthelid M., Grehk T.M., Karlsson U.O., 1998. NH3 on Si(111)7x7: Dissociation and surface reactions. Physical Review B 57, 2327–2333.
Chen P., Wu X., Sun X., Lin J., Ji W., Tan K.L., 1999. Electronic Structure and Optical Limiting Behavior of Carbon Nanotubes. Physical Review Letters 82, 2548–2551.

Ciraci S., Dag S., Yildirim T., Gülseren O., Senger R.T., 2004. Functionalized carbon nanotubes and device applications. Journal of Physics: Condensed Matter 16, R901–R960.
Collins P.G., Bradley K., Ishigami M., Zettl A.,2000. Extreme oxygen sensitivity of electronic properties of carbon nanotubes. Science 287, 1801–1804.

Drube W., Schulte-Schrepping H., Schmidt H.-G., Treusch R., Materlik G., 1995. Design and performance of the high-flux high-brightness X-ray wiggler beamline BW2 at Hasylab. Review of Scientific Instruments 66, 1668–1670.
Drube W., Grehk T.M., Treusch R., Materlik G., 1998. Tunable high-energy X-ray photoemission. Journal of Electron Spectroscopy and Related Phenomena 88, 683–687.
Felten A., Bittencourt C., Pireaux J.-J., Van Lier G., Charlier J.C., 2005. Radio-frequency plasma functionalization of carbon nanotubes surface O-2, NH3, and CF4 treatments. Journal of Applied Physics 98, 074308.
Hammer P., Lacerda R.G., Droppa R., Alvarez F., 2000. Comparative study on the bonding structure of hydrogenated and hydrogen free carbon nitride films with high N content. Diamond and Related Materials 9, 577-581.
Johnson R.L., Reichardt J., 1983. Flipper II – a new photoemission system in Hasylab. Nuclear Instruments and Methods in Physical Research 208, 791–796.
Khare B.N., Wilhite P., Quinn R.C., Chen B., Schingler R.H., Tran B., Imanaka H., So C.R., Bauschlicher Jr. C.W., Meyyappan M., 2004. Functionalization of carbon nanotubes by ammonia glow-discharge: Experiments and modeling. Journal of Physical Chemistry B 108, 8166–8172
Lim S.C., Jo C.S., Jeong H.J., Shin Y.M., Lee Y.H., Samayoa I.A., Choi J., 2002. Effect of oxidation on electronic and geometric properties of carbon nanotubes. Japanese Journal of Applied Physics 41, 5635–5639.
Ruelle B., Peeterbroeck S., Gouttebaron R., Godfroid T., Monteverde F., Dauchot J.-P., Alexandre M., Hecq M., Dubois Ph., 2007. Functionalization of carbon nanotubes by atomic nitrogen formed in a microwave plasma Ar+N2 and subsequent poly(e-caprolactone) grafting. Journal of Materials Chemistry, 17, 157–159.
[image: image1.emf] 

(a )  


Figure 1: SEM image of MWCNTs treated in the post-discharge region of an Ar-N2 microwave plasma
[image: image3.emf]300 295 290 285 280

 

 

 

Binding Energy (eV)

Intensity (arb. units)


Figure 2: HRTEM image of MWCNTs treated in the post-discharge region of an Ar-N2 microwave plasma.
[image: image4.png]



Figure 3: Overview XPS spectra a) pristine MWCNTs  b) MWCNTs exposed to atomic nitrogen flow in the post-discharge region for 15 minutes. The inset shows the XPS N 1s spectrum.
[image: image5.emf]500 400 300 200 100 0

 

 

 

Binding Energy (eV)

Intensity (arb. units)

408 404 400 396 392

 


Figure 4: XPS C 1s spectra recorded on a) pristine CNTs and b) atomic-nitrogen treated CNTs.
[image: image6.emf]20 15 10 5 0

 

 

 

Binding Energy (eV)

Intensity (arb. units)


Figure 5: Valence band spectra recorded on pristine MWCNTs (a) and MWCNTs exposed to atomic nitrogen produced by MW Ar-N2 plasma for 5 minutes (b), 15 minutes (c), and 30 minutes (d). Horizontal arrows indicate the extension of the valence band states whereas vertical arrows indicate the reported calculated value (Hammer et al., 2000). 
[image: image8.jpg]


[image: image2.emf] 

b)  


C-C σ states





C-C π states











N 1s

















b)








a)








C 1s





d)





c)





b)





C 1s





a)








C-N π states





  C-N σ states

















� Corresponding author: Tel: +3265373851, e-mail: carla.bittencourt@materianova.be





[image: image7.jpg]


